# Text boxes

Product Information

DuPontTM 959G-2XX

Industrial Nonstick Coatings

DuPontTM industrial coatings 959G-2XX are solvent based, one coat, fi nishes designed for use under moderate abrasion and where nonstick properties contribute to product performance. These nonstick fi nishes are designed for moderate cure temperature and the coatings can also be used as primers.

One Coat

959G-203

One Coat

959G-204

One Coat
959G-205

Property Data

Product Code

Dark Brown

7.9 (336)

800 – 1200

16.4 – 18.4

26.3 – 29.3

1.04 (8.72)

220 (425)

–100L

YES

Black

7.7 (319)

800 – 1200

16.0 – 18.0

23.0 – 26.0

1.02 (8.57)

220 (425)

–100L

YES

Green

8.3 (351)

800 – 1200

16.3 – 18.3

26.5 – 29.5

1.04 (8.69)

220 (425)

–100L

NO

Properties1 Color

Coverage,2 m2/kg (ft2/gal)

Viscosity,3 centipoises

Volume Solids, %

Weight Solids, %

Density, kg/l (lbs/gal)

Maximum In-Use Temperature, °C (°F)

Shipping Class

Food Contact Compliance

1 Physical constants are averages only and are not to be used as product specifi cations. They may vary up to 5% of the values shown

2 Theoretical coverage at dry fi lm thickness (DFT) of 1.0 mils (25µ) based on 100% application effi ciency. It does not take normal production losses into account

3 Brookfi eld RVT (Measured with spindle 2 at 20 RPM/25 °C)

Application Method

Any metal substrate except high copper containing alloys

Degreasing, gritblasting is recommended, but not required. Pre-bake metal 15 min. at 343 °C (650 °F).

Apply over clean, roughened surface. Application to food contact approved conversion coatings is suggested where grit blasting is not practical. Any residual oil on the surface will affect the color of the cured fi lm and will adversely affect adhesion.

Stir well before use. Roll or mix with a propeller-type mixer until contents are homogeneous.

Strain through 150-mesh wire screen or cheese cloth.

Use conventional industrial spray equipment. Agitate during use of sprayed from a pressure pot.

Manual or Automatic Spray: No reduction required. If lower viscosity is desired, reduce with TN-8595, NMP or MIBK.

Film Thickness 15–30 µm (0.6–1.2 mil) DFT per coat.

These products are recoatable. Maximum DFT in multiple coats: 64 µm (2.5 mil). One Coat System

Flash dry in air 1–5 min. prior to bake. Note: If humidity is 85% or above, do not air fl ash. Instead, place in oven immediately to minimize absorption of moisture which may cause pinholes and water blisters.

Bake 15 min. at 150 °C (300 °F), followed by 15 min. at 345 °C (650 °F) Multiple Coats

For dry fi lm builds greater than 30 µm (1.2 mil), bake initial coat and any intermediate coats: 15 min. at 150 °C (300 °F) Final bake: 15 min. at 345 °C (650 °F)

TN-8595
TN-8595

Substrate

Substrate Preparation

Coating Preparation

Filtering Application

Recommended DFT

Curing (Metal Temperature)

Clean up Thinner/Additive

All recommendations are based upon best knowledge

Handling and Storage *

- Storage life is 18 months maximum at room temperature.

- Storage temperature 18–27 °C.

- Roll for 30 minutes at 30 RPM once per month.

- Warm containers to room temperature and roll completely before use.

- Solvent-based product

- For medical application and development, please consult DuPont.

Food Contact

959G-203 and 959G-205 coatings are designed to be used in direct contact with food. Applied according to the below

application method and instructions, the fully cured coating will comply with US FDA food contact regulations, 21.CFR, and can be sold and/or used for food contact applications for nonstick coatings in Europe following the national legislations of each European country, having specifi c regulations for this category of coatings (nonstick, high temperature resistant).

Any changes or variations of individual coating thickness from what is indicated in this fact sheet should be assessed for food contact applications prior to its use. For details and information please contact your DuPont representative.

- Incinerate only if incinerator operates at 800 °C or higher and is capable of scrubbing out hydrogen fl uoride and other acidic combustion products.

- Industrial fl uoropolymer waste containing additives such as solvents, primers or thinners must be regarded as special waste. Companies should contact their local waste disposal authorities for details of the relevant waste disposal regulations.

- Empty containers should preferably be cleaned and recycled. If this is not possible, the containers should be punctured or otherwise destroyed before disposal.

For detailed information on health and safety, refer to the Material Safety Data Sheet and the latest edition of “The Guide to the Safe Handling of Fluoropolymer Resins,” published by The Society of the Plastics Industry, Inc. (www.fl uoropolymers.org) or by PlasticsEurope (www.plasticseurope.org).

959G-204 is NOT food contact compliant in the United States.

Disposal and Other Considerations

Please follow these guidelines as outlined in the “ Safety Handling Guidelines for Fluoropolymers.”

For disposal, please follow these guidelines:

- All treatment, storage, transportation, and disposal of this product and/or container must be in accordance with applicable national and local regulations.

- Do not discharge aqueous dispersions to lakes, streams or waterways.

- Separate solids from liquid by precipitation and decanting or fi ltering. Dispose of dry solids in a landfi ll that is permit ted, licensed or registered to manage industrial solid waste. Discharge liquid fi ltrate to a wastewater treatment system.

For more information on

DuPont Industrial Nonstick Coatings, please visit www.tefl on.com/industrialglobalsupport

DuPont

Wilmington, Delaware, USA

Phone: U.S. callers: 1-866-205-1664

Fax: (302) 351-7264

P.O. Box 80702

Wilmington, DE 19880-0702

Copyright© 2011 DuPont. All rights reserved. The DuPont Oval Logo, DuPontTM, The miracles of scienceTM, and Tefl on® are registered trademarks or trademarks of E.I. du Pont de Nemours and Company or its affi liates.	K-24266 10/11

Tefl on® is a registered trademark of E.I. du Pont de Nemours and Company, only available for use under license and subject to qualifi cation.

NO PART OF THIS MATERIAL MAY BE REPRODUCED, STORED IN A RETRIEVAL SYSTEM OR TRANSMITTED IN ANY FORM OR BY ANY MEANS ELECTRONIC, MECHANICAL, PHOTOCOPYING, RECORDING OR OTHERWISE WITHOUT THE PRIOR WRITTEN PERMISSION OF DUPONT.

All technical advice, recommendations and services are rendered by Seller free of charge. They are based on technical data which the Seller believes to be reliable, and are intended for use by persons having skill and know-how, at their own discretion and risk. Seller assumes no responsibility for results obtained or damages incurred from their use by Buyer in whole or in part. Such recommendations and technical advice or services are not to be taken as a license to operate under or intended to suggest infringement of any existing patent. All coverage fi gures are based on 100% application effi ciency. These calculations do not take into account normal losses due to production conditions.

CAUTION: Do not use DuPont materials in medical applications involving implantation in the human body or contact with internal body fl uids or tissues unless the material has been provided from DuPont under a written contract that is consistent with DuPont policy regarding medical applications and expressly acknowledges the contemplated use. For further information, please contact your DuPont representative. You may also visit www.tefl on.com/industrial to download a copy of the DuPont POLICY Regarding Medical Applications H-50103 and DuPont CAUTION Regarding Medical Applications H-50102.